## Slide 1: Nanoscale thermal transport
Lecture 1
Riley Hanus
http://rileyhanus.com/science.html

## Slide 2
Two rules
Use your imagination
  You should be actively building a picture in your head.
  I’ll do my best to provide good pictures, but the pictures will fall short.
  2. Don’t be afraid of the math
  It’s (almost) impossible to know every bit of math that is thrown at you.
  You will need to learn math as you go.
  All math can be learned, it just might take some patience.

## Slide 3
Define thermal conductivity,
Overview of heat conduction mechanisms
  electrons
  bipolar
  atomic vibrations
Define (and understand) temperature
Define (and understand) reciprocal space
  First Brillouin Zone
  Band structures
600K

## Slide 5
Fourier’s Law
vector notation:
Einstein notation:
: heat flux (3x1 vector)
: thermal conductivity (3x3 matrix)
: gradient of temperature (3x1 vector)
Let’s be explicit:

## Slide 6
For a cubic material is isotropic, even though elastic properties, speed of sound, and phonon dispersion is not!
Young’s Modulus contour of Si from Materials Project
Why?
is the result of an integration over the first Brillouin zone (FBZ)
This will make more sense after we cover reciprocal space.

## Slide 7
Einstein (index) notation
Rule: sum over repeated indices in a term, sometimes called a ‘dummy’ index
Why worry about Einstein notation?
Einstein notation makes tensor math much cleaner and is really the best (only?) way to do tensor math in dimensions higher than 3 (tensors rank 4 and up).
Elastic properties (involves 4th rank tensors) Thermal properties

## Slide 8
What conducts heat?
Electrons (Wiedemann-Franz Law)
: electrical conductivity
: Lorenz number
Band modeling for better estimation of in semiconductors, and a simple formula for it:
Kim, H.-S., et al. Characterization of Lorenz number with Seebeck coefficient measurement. APL Mater. 3, 041506 (2015).
For metals and degenerate semiconductors
(worth remembering)
Note:
Depends on electronic band structure
Varies in semiconductors, but typically no more than 20%
This value held for doped, metallic like conducting polymer PEDOT:PSS
Weird things happening in VO2

## Slide 9
What conducts heat?
Bipolar conduction:
in the intrinsic regime
Occurs when electronic conduction is happening in both conduction and valence bands
Absorb heat
Release heat
Paper discussing bipolar thermal conductivity, lots of good references:
Bahk, J. H. & Shakouri, A. Appl. Phys. Lett. 105, 6–11 (2014).
At 300 K

## Slide 10
Aside: Electronic band structure of Si from DFT, Materials Project
Si bandgap is 1.1 eV
DFT usually gets the band gap wrong
Anything wrong?

## Slide 11
What conducts heat?
Atomic vibrations:
Interatomic force constants (IFCs)
  think ball and spring
IFCs atomic masses structure
normal modes of vibration
Phonons!

## Slide 12
What is temperature?
Measure of ‘hotness’.
Temperature () of a ‘state’ at energy in a material is given by its occupation number .
If the ‘state’ represents a boson, we use the Bose-Einstein distribution.
If I know the energy of all states and the number of (quasi-) particles in those states , I know

## Slide 13
What is temperature?
300 K
Diffuse
600K
sufficient coupling between states
Coupling → phonon lifetime, relaxation time, mean free path

## Slide 14
What is temperature?
600K
600 K
But we are still pumping heat through, !
What’s going on?
Fourier’s law breaks down for ballistic transport!
(I say not defined, some will say )
Ballistic
‘Effective’ is lower in ballistic transport than it is in diffuse

## Slide 15
Reciprocal space
k-space
Why do we work in reciprocal space?
It’s more natural to examine waves in reciprocal space.
Can you tell me what this waveform sounds like? NO
Once you see its Fourier transform in reciprocal space? MAYBE

## Slide 16
Reciprocal space
k-space
Let’s apply the same concept to a crystal
Start in 1D
a
(lattice parameter)
time frequency space wavelength reciprocal space
The crystal structure will set a minimum , or a maximum
2a

## Slide 17
Reciprocal space
k-space
Defining the First Brillouin Zone, FBZ
(pronounced BREE – you – on with a soft ‘n’, its French)
See Kittle, Introduction to Solid State Physics, pg. 26 to 41
Step 1
Start with unit cell vectors:
and
(typically we work with primitive unit cells)
volume:
Step 2
Define reciprocal lattice vectors:
, ,
Note: be mindful of your ’s. Some define k-space with , a lot of codes don’t.
analogous to
Step 3
Draw planes halfway between each reciprocal lattice point
FCC

## Slide 18
Reciprocal space
k-space
Defining the First Brillouin Zone, FBZ
Step 4
Give certain k-points fancy names
Step 5
Walk from point to point and map energies of phonons, or electrons
What’s the wavelength at ? What about X?
You can think of a phonon band structure (roughly) as the Fourier transform of the interatomic spring constants, weighted by the atomic masses.
https://www.cryst.ehu.es/

## Slide 19
Phonon band structures
Most solid-state physics classes will derive an analytical dispersion for a 1D chain.
If you haven’t seen this, read Kittel, Intro. to Solid State physics Chapter 4.
Much of the intuition gained from the 1D case extends to 3D
The math for a 3D crystal, which is used to calculate real dispersion relations is given in:
Wallace, Thermodynamics of Crystals, Chapter 3.10.
Hanus, Thesis, Section 2.2.1 and Appendix B.
Here we will outline the procedure for computing phonon properties:
frequencies
eigenvectors
(mode shape)

## Slide 20
Phonon band structures
Simply solve the equations of motion (Newton’s law)
: atom label
: direction
We know and ,
solve for .
Databases for interatomic force constants (IFCs) :
Phonopy: http://phonondb.mtl.kyoto-u.ac.jp/
almaBTE: http://www.almabte.eu/index.php/database/
Set up

## Slide 21
Phonon band structures
Expressing a function as a Fourier Series
1. Express as a Fourier Series
2. Solve equation of motion ()
2a. In solving we find its convenient to define the Dynamical Matrix
2b. Phonon ’eigenstates’ are the solutions you get when you diagonalize the Dynamical Matrix
scalar
3n length vector
3n x 3n matrix
3n length vector
distinct and
solutions

## Slide 22
scalar
length vector
matrix
length vector
distinct and solutions
= # of atoms in unit cell

## Slide 23
Phonon band structures
In practice
Find solutions (diagonalize the Dynamical Matrix)
Along special directions to plot
pretty band structures:
On a mesh to sample the entire Brillouin Zone, when we want transport properties of density of states:
Computational suites that do this:
phonopy: https://atztogo.github.io/phonopy/
almaBTE: http://www.almabte.eu/
shengBTE: http://www.shengbte.org/

## Slide 24
Reading a phonon band structure
acoustic modes ( at )
optical modes ( at )
where is the number of atoms in the unit cell
Ultrasound, speed of sound,
Elastic tensor and moduli,
Bulk modulus, Young’s modulus,
etc.

## Slide 25
Reading a phonon band structure
Group velocity

## Slide 26
Reading a phonon band structure
Effect of atomic mass and the
phonon band gap.
Cubic GaN
Cubic GaAs
25 meV
25 meV

## Slide 27
Resources
https://www.cryst.ehu.es/
space-group symmetry
  KVEC
  type in space group # (FCC Si, Fd-3m, no. 227)
  click Brillouin zone
Phonon simulation software and databases:
phonopy: https://atztogo.github.io/phonopy/
almaBTE: http://www.almabte.eu/
shengBTE: http://www.shengbte.org/
Elastic properties:
Elastic tensors: materials project
averaging: https://github.com/JanJaeken/christoffel