## Slide 1: Nanoscale thermal transport
Lecture 4
Riley Hanus
http://rileyhanus.com/science.html

## Slide 2
A breakdown of phonon thermal conductivity
The vibrational (lattice) Hamiltonian
  The Harmonic Hamiltonian
  Types of phonon scattering
Scattering potential → Scattering Probability → Relaxation time (lifetime)
  point defects
  line defects
  planar defects
Phonon-phonon scattering
Low-frequency behavior of thermal conductivty

## Slide 3
Phonon scattering and thermal conductivity
: kinetic energy of all atoms
: potential energy of all atoms expressed as a Taylor expansion

## Slide 4
Hamiltonian
Energy of a solid is described by its Hamiltonian,
: kinetic energy of all atoms
: potential energy of all atoms
PE = ???
Taylor expand it:
reference energy, set this to zero
linear term is zero when all atoms are in their equilibrium positions
on board

## Slide 5
Hamiltonian
Energy of a solid is described by its Hamiltonian,
: kinetic energy of all atoms
: potential energy of all atoms
on board

## Slide 6
Harmonic Hamiltonian
distinct and solutions
Allows us to write this equation of motion:

## Slide 7
Types of perturbations
Mass (density) changes
Spring constant changes
Changes in strain

## Slide 8
Types of perturbations
Phonon-phonon scattering
Mass contrast scattering
Bond strength contrast scattering

## Slide 9
Types of perturbations
Static strain field scattering

## Slide 10
Scattering potential → relaxation time
on board
You can find reference’s in R. Hanus’ thesis Appendix G or Ashcroft and Meremin pg. 316
Probability of scattering from state k into k’ given by Fermi’s Golden Rule:
I) is the sum over all possible k’ states.
inverse lifetime:
What if k = k’ ? Does this scattering event impede heat conduction?
inverse relaxation time
or scattering rate:
isotropic approximation, this becomes
See detail on Relaxation Time Approximation in supplemental slides

## Slide 11
Contributions to the relaxation time
Codimension:
Example:
line defect is 1D.
Need 2 dimensions to define it.
Mathematically this looks like:
spatial density of defects
Phase space contribution:
Density of states into which the phonon can scatter.
Matrix element contribution:
Magnitude squared of the Fourier transform of the scattering potential
Elastic defect scattering can be expressed as the product of the three factors.

## Slide 13
Scattering theory
Integral definition of the Dirac -function
Some -function identities:
where at
Example:
Required Math
on board

## Slide 14
Scattering theory
The square of a Dirac -function
Required Math
on board
Note: In the following examples we are building intuition about phase space and matrix element contributions and therefore we apply a ‘spectral’ treatment of scattering theory, making the isotropic single mode approximation.
Aside: Mode specific treatments can be done by expressing the factors of in in terms of creation and annihilation operators (Eq. L.14 in Ashcroft and Mermin) and computing the matrix element by following the creation and annihilation operator rules:
creation operator:
creation operator:

## Slide 15
Point defect – Mass contrast
on board
: volume of solid containing one defect who’s scattering potential is given by .
: volume of defect
Normalized plane wave:
Scattering vector:

## Slide 16
Point defect – Mass contrast
on board

## Slide 17
Point defect – Mass contrast
we set k to be in the z-direction so (angle between k and k’) equals the polar angle of k’ in spherical coordinates.
’
on board

## Slide 18
Point defect – Mass contrast
A localized scattering potential ( in ) results in . The fact that it’s a point defect (0d, ), means the phonon can scattering into the 3D density of states, . Together we get the Raleigh scattering, power law.

## Slide 19
Line defect – Mass contrast
A localized scattering potential ( in ) results in . The fact that it’s a line defect (1d, ), means the phonon can scattering into the 2D density of states, . Together we get the power law.
details in supplemental slides

## Slide 20
Elastic defect scattering cheat sheet
0D (point defect, )
1D (line defect, )
2D (planar defect, )

## Slide 21
Phonon-phonon scattering
Type II:
two phonons combine into one
Type I:
one phonon decomposes into two
: any reciprocal lattice vector
Normal scattering process:
Umklapp (“flip over”) scattering process:
Perturbation is
and are initial and final states (combinations of k1 k2 and k3)
Maznev, A. A. & Wright, O. B. Demystifying umklapp vs normal scattering in lattice thermal conductivity. Am. J. Phys. 82, 1062–1066 (2014).

## Slide 22
Phonon-phonon scattering
Phonon-phonon scattering has phase space and matrix element contributions as well.
weighted joint density of states
average anharmonic interaction phonon has with all other phonons
Togo, A., Chaput, L. & Tanaka, I. Distributions of phonon lifetimes in Brillouin zones. Phys. Rev. B 91, 094306 (2015).
contains the number of other phonons in the material
at high temperature
Stems from high-T behavior of Bose-Einstein distribution
at high temperatures

## Slide 23
Phonon-phonon scattering
Common analytical form:
Low- behavior from DFT based lattice dynamics and phonon-phonon relaxation time.
Si
300K
GaN
300K
lines show
with

## Slide 24
Phonon-phonon scattering
Analytical high-T phonon-phonon scattering model
Toberer, E. S., Zevalkink, A. & Snyder, G. J. Phonon engineering through crystal chemistry. J. Mater. Chem. 21, 15843 (2011).
Fully analytical thermal conductivity model using the above phonon-phonon scattering expression shows reasonable agreement with experiment across two orders of magnitude.
Good for broad screening across material systems.

## Slide 25
Low frequency behavior of spectral thermal conductivity
as

## Slide 26
BZ integration and k-meshing
Si at 300K
12x12x12

## Slide 27
Si at 300K
16x16x16
BZ integration and k-meshing

## Slide 28
Si at 300K
20x20x20
BZ integration and k-meshing

## Slide 29
Si at 300K
30x30x30
BZ integration and k-meshing

## Slide 30
T 3
T -1
Low-T gives information about grain boundary scattering
High-T, behavior stems from phonon-phonon scattering
Example Callaway model
Notes: Check units!!

## Slide 31
Relaxation time approximation
supplemental
Phonon-gas model for heat flux:
compare to solve for
need , get it from BTE

## Slide 32
Relaxation time approximation
Boltzmann transport equation (BTE)
no external forces on phonons
Left side:
Only spatial (real space gradient) dependence of
is through spatial dependence of T
suppress
Right side:
Time dependence only through
Making the Relaxation Time Approx.
supplemental

## Slide 33
Relaxation time approximation
supplemental

## Slide 34
Relaxation time and dispersion relation line width
Vibrational amplitude as a function of time:
Real part and magnitude squared () of Fourier transform are a Lorentzian function with FWHM =
long
short
Note: has same units as
supplemental

## Slide 35
Line defect – Mass contrast
supplemental
: cross-sectional area of line defect

## Slide 36
Line defect – Mass contrast
since this is multiplied by , we can pull out the
supplemental

## Slide 37
Line defect – Mass contrast
Can take the integrals over and
with
supplemental