## Slide 1: Nanoscale thermal transport
Lecture 3
Riley Hanus
http://rileyhanus.com/science.html

## Slide 2
General discussion about heat capacity
Obtain the phonon heat capacity
  examine limiting behavior
  low , high T, low T
Heat capacity in practice
  Debye level
  Debye temperature
  Speed sound
Introduction to scattering theory

## Slide 3
Heat capacity is generally a very boring material property.
Heat capacity
Material | Volumetric heat capacity at 25 C
Liquid Hg | 1.9
Liquid water | 4.2
Cu | 3.45
Glass | 2.1
Al | 2.4
Graphite | 1.53
Diamond | 1.8
Material | 
Liquid Hg | 1.9
Liquid water | 4.2
Cu | 3.45
Glass | 2.1
Al | 2.4
Graphite | 1.53
Diamond | 1.8

## Slide 4
constant
: number density of atoms
: Gruneisen parameter
: volumetric thermal expansion ()

## Slide 5
Derivation set-up
Heat capacity is the change in energy with temperature
We will look for the spectral heat capacity per unit volume
Energy density:
Number density of phonons:
Note:
is the number of possible states per unit volume. Here, we say it doesn’t change with temperature (i.e. the quasi-harmonic approximation). In reality thinks get softer with increasing temperature so will shift down in as increases.
is the occupation number (can think of it as an occupation probability), of a state at frequency/energy , and temperature .
on board

## Slide 6
Derivation
Crazy triple chain rule
Heat capacity per volume
on board

## Slide 7
Limiting behavior
Let’s look at the low (and high T) behavior
If I just plug in .
Not super helpful, what we really want is the limiting behavior.
At high T and or low
which means at high T
and when the dispersion is linear
Define:
Taylor expand about .
on board

## Slide 8
Limiting behavior
Let’s look at low behavior
Convenient to convert the integral to be over the dimensionless parameter .
At low T:
only low frequency modes are populated,
At low T
where dispersion is linear:
on board

## Slide 9
Example model
constant
speed of sound:
volume per atom: (: volume of unit cell, : # atoms in unit cell)
max k-vector (isotropic):
Debye frequency:
Debye temperature:
on board

## Slide 10
Analyzing low-T data
good
exercise
: number density of atoms
Agne, M. T. et al. Heat capacity of Mg3Sb2, Mg3Bi2 and their alloys at high temperature. Mater. Today Phys. 6, DOI 10.1016/j.mtphys.2018.10.001 (2018).

## Slide 11
Speed of sound
When the cross-correlation is used to measure the time delay, the error is typically limit by the thickness variation of the sample. Can get better than 1% accuracy, if careful.
If sample is a randomly oriented polycrystalline, then you are measuring the isotropic average longitudinal and transverse speeds of sound.
Be mindful of preferred orientation of grains, especially for non-cubic materials.
Be mindful of sample density. Samples should be very dense, >98%.
The isotropic average speed of sound, used for thermal conductivity modeling, heat capacity modeling, Debye temperature.
Anderson, O. L. A simplified method for calculating the Debye temperature from elastic constants. J. Phys. Chem. Solids 24, 909–917 (1963).

## Slide 12
Thermal expansion contribution
: number density of atoms
: Gruneisen parameter
: isothermal Bulk modulus
: volumetric thermal expansion ()

## Slide 13
Analyzing high-T data
Absolute value of high temperature heat capacity is notoriously hard to measure.
In contrast low-temperature heat capacity can be very accurate (e.g. physical property measurement system PPMS in heat capacity mode).
Often times our models are better at predicting it then and one given measurement is.
The slope of Heat Capacity vs. T at high T can be reasonably accurate.
Agne, M. T. et al. Heat capacity of Mg3Sb2, Mg3Bi2 and their alloys at high temperature. Mater. Today Phys. 6, DOI 10.1016/j.mtphys.2018.10.001 (2018).

## Slide 14
Thermal conductivity considerations
Modeling:
: spectral heat capacity per unity volume
: spectral diffusivity
Experiment:
: thermal diffusivity measured by, for example LFA
: heat capacity per unit volume
: heat capacity per unit mass
: mass density
on board
Heat capacity weighted average diffusivity